Specific Heats (J / kg C)

Solids

Aluminum		900

Copper			387

Glass			840

Ice			2000

Iron or Steel		452

Lead			128

Silver			235

Human Body (37 C)	3500

Liquids

Alcohol (Ethyl)		2450

Glycerin		2410

Mercury		139

Water			4186

Gasses

Carbon Dioxide		2190

Oxygen			912

Water Vapor		2020

Index of Refraction

Solids @ 20˚C

Diamond		2.419

Glass, crown		1.52

Ice (0˚C)		1.309

Sodium Chloride	1.544

Quartz

Crystalline	1.544

Fused		1.458

Liquids @ 20˚C

Benzene		1.501

Carbon

Tetrachloride	1.461

Ethyl Alcohol		1.362

Water			1.333

Liquids @ 0˚C, 1 atm

Air			1.000 293

Carbon Dioxide		1.000 45

Oxygen, O2		1.000 271

Hydrogen, H2		1.000 139

Constants

Acceleration of Gravity:

Earth:	9.8 m/s2	32 ft/s2

Moon: 1.6 m/s2	5.33 ft/s2

Universal Gravitational Constant

6.67 x 10-11 Nm2/kg2

Electromagnetic Spectrum